VIET KAI ECOTECH COMPANY LIMITED

PRODUCT SPECIFICATIONS

DESCRIPTION: FABRIC _VKF642 No.; TECHNICAL FACTORS; SPECIFICATIONS. 1; Brand; VIET KAI. 2; End use; Upholstery. 3; Characteristics; Cut Pile Jacquard Weave. 4; Design type; Embossing Process. 5; Repeats; V:Embossing Process H: Embossing Process. 6; Composition; 100% Polyester. 7; Abrasion (Martindale); More than 30.000 Rub. 8; Useable width in cm; 142.00 (56 inch). 9; Weight in gsm; 420 GSM. 10; Tear Strength (N); L:27N ; W:40N. 11; Seam Strength (N); L:1mm ; W:1mm 200N. 12; Tensile Strength (N); L: 550N ; W: 800N. 13; Colour Fastness to light; 4. 14; Pilling; 4. 15; Care code for washing (°C); Wash at 30°C gentle cycle. 16; Care code for dry cleaning; Dry-cleaning in perchloroethylene gentle cycle. 17; FR standard; American CAL 117. 18; Certificate; OKEX-TEX STANDARD 100, SGS, GRS,... 19; Uses of goods; Furniture.